## Slide 1
David Harris
Harvey Mudd College
David_Harris@hmc.edu
Based on EE271 developed by Mark Horowitz, Stanford University

## Slide 2: Overview
Reading
  W&E 3.1, 3.2.1-3.2.3, 3.3.1 - Fabrication
  W&E 3.4-3.4.3 - Design Rules
    ( rules are really not that bad)
Introduction
The whole IC business is based on the fact that complex circuits can be ‘printed’ on a silicon wafer, thus the cost of the chip depends mainly on its size and not the number of devices (the complexity of the picture). This fabrication process is possible because of special properties of semiconductors and in particular the semiconductor silicon. This lecture will briefly review some semiconductor properties, and then describe how chips are made. The fabrication discussion will motivate the design rules that need to be followed for layout.

## Slide 3: What Do We Need to Build?
Transistors
Need NMOS and PMOS
How are these built?
Wires
Many levels of real metal wires (mostly aluminum or copper)
  We we see that we need low resistance (high conductivity)
Oxide (SiO2) insulator between metal layers
Contacts (hole in the oxide) between adjacent layers
  Adjacent layers only
  To connect M1 to M3, need to connect M1 to M2, and M2 to M3
Let’s digress and look at how to build a transistor
  Physics, and materials

## Slide 4: + Silicon
IC fabrication depends on two properties of silicon:
It is a semiconductor
  Conductivity can be changed by adding impurities
  These impurities, called dopants, can create either n-type or p-type regions.
Its oxide is very stable
  It is SiO2 , which is quartz or glass (amorphous)
    ‘silicon rust’ is glass
  Great for sealing stuff from impurities
  Can be selectively patterned.
  Etching can remove SiO2 without harming Si.
  Stable grown oxide is the great advantage of Si over Ge or GaAs.

## Slide 5: + Doping
Adding arsenic or phosphorous to the intrinsic silicon increases its conductivity by adding ‘free’ electrons. Silicon with electron carriers is called n-type silicon, since the current is carried by particles with negative charge.
Adding boron to intrinsic silicon increases its conductivity by adding ‘free’ holes. Holes are like electrons, but have a positive charge, so this type of material is called p-type silicon.
The junction between n-type and p-type regions have special properties – it forms a diode.
Note that the doping also adds fixed charge in addition to the mobile charge so the region remains neutral. n doping adds fixed positive charge and mobile electrons, and p doping is fixed negative charge and mobile holes

## Slide 6: +How to Build a Transistor
Diffusion is made by adding (diffusing) impurities into the silicon
n+(p+) diffusion means the region has a lot of impurities (dopants) which improves it conductivity (and hence lowers its resistance)
p (n) regions are more lightly doped
p region is formed first, and then the n+ over dope parts of the p region to form the n+ regions
n+ dopant is added after the poly is down so poly blocks dopant
n+
n+
poly
p

## Slide 7: CMOS Has Two Transistor Types
CMOS devices require two types of substrate for isolation of transistors
n-type for PMOS
p-type for NMOS

## Slide 8: Wells: Local Substrates
Fabricators can choose to make the base wafer n-type (add pwells) or p-type (add nwells), or choose to add both, (“twin” wells).

## Slide 9: Well Requirement
Well must to be tied to a power supply to keep the isolation diodes reversed biased. This is accomplished by using well contacts.

## Slide 10: - Well Contacts
Formed by placing p+ doped region in a pwell
or n+ doped region in a nwell
These regions make good electrical contact (ohmic, not diode) to the well and thus the well potential is made equal to the potential of the diffusion.
Need to have at least one well (substrate) contact in each well.
These contacts are then connect to the correct power supply to ensure that the diodes are always reversed biased.

## Slide 11: What is On a Chip
Transistors
Requires silicon substrate, wells
Diffusion (two types), poly
Wires
Many levels of real metal wires (mostly aluminum)
Oxide insulator between metal layers
Contacts (hole in the oxide) between adjacent layers
Now that we have a quick overview of what we are building, lets delve in more detail into how to build it.

## Slide 12: Fabrication
The process used that creates these devices/wires.
Look at how to create:
  Working transistors
    ndiff, pdiff, wells, poly, transistors, threshold adjust implants
  Wires
    contacts, metal1, via, metal2
Fabrication is pretty complex.
There are whole classes devoted to it (grad school!).
Give a brief overview of the process, for background.
Want to understand origin of layout rules / process parameters
  The abstractions of the process for the designer (us).

## Slide 13: Making Chips
Wafers
Processing
Chemicals
Processed Wafer
Chips
Masks

## Slide 14: + Basic Fabrication Step
Two parts:
Transfer an image of the design to the wafer
Using that image as a guide, create the desired layer on silicon
  diffusion (add impurities to the silicon)
  oxide (create an insulating layer)
  metal (create a wire layer)
Use the same basic mechanism (photolithography) to do step 1.
Use three different methods to do step 2.
Ion Implant - used for diffusion. Shoot impurities at the silicon.
Deposition - used for oxide/metal. Usually from chemical vapor (CVD)
Grow - used for some oxides. Place silicon in oxidizing ambient.

## Slide 15: Basic Processing
Start with wafer at current step
Spin on a photoresist
Pattern photoresist with mask
Step specific processing etch, implant, etc...
Wash off resist

## Slide 16: - Integrated Circuit Fabrication
Repeat:
  Create a layer on the wafer*
  Put a photo-sensitive material (resist) on top of the wafer
  Optically project an image of the pattern you desire on the wafer
  Develop the resist
  Use the resist as a mask to prevent the etch (or other process) from reaching the layer under the resist, transferring the pattern to the layer
  Remove the resist
Key point is that all the chips (die) on the wafer are processed in parallel, and for some chemical steps, many wafers are processed in parallel.
* For some layers (diffusion, well) the ‘stuff’ is added after the resist, so the resist only allows the impurities to go where they are desired. For most other layers (oxide, metal) the entire surface is covered first, and then the ‘extra’ material is removed.
Sometimes the layers don’t always correspond to the exact same layers designers think about.

## Slide 17: + Photolithography
To transfer the pattern onto the wafer, one first needs to have an image to project. While this can be done using some scanning technology directly from the design database to the wafer (like generating a TV picture), it is usually done using a two step process:
  First a glass plate with a image of the pattern etched in chrome is generated from the design database. This glass plate is called a mask, and serves the same function of a negative in photography.
  This image is optically projected onto wafer using a “projection-aligner” which is very much like an enlarger in photography. It projects the image of the mask onto the silicon wafer. Resolution is impressive.
This two step process is used since scanning data serially is an expensive step since it takes a long time on an expensive machine. By generating a mask which can print on a large number of wafers, the cost per wafer can be made small. (But implies that you want lots of parts).

## Slide 18: + Mask (Reticle) Manufacture
MEBES format and machine, or others
Place a glass plate covered with chrome covered with resist in a high-vacuum column
Use an electron beam spot size smaller than the finest resolution of your design.
Scan the surface of the mask with the e-beam in a raster-scan order. Modulate the beam to transfer the pattern to the chrome
Develop the resist, and the chrome, and then remove the resist
Check and correct the chrome pattern.
.
.
.
.
All modern processes use masks (reticles) that are 5-10x larger than the desired size. The mask aligners then project the image and reduce it in the projection. While this means that exposing a wafer takes multiple prints, it is needed to reach the resolutions needed (< 1) for current technologies.

## Slide 19: Making Transistors
1. Implant N-Well
2. Define thin oxide grow field oxide, implant doping to adjust transistor threshold
3. Deposit and etch polysilicon
The threshold adjust implant is doping added under the gates of the transistors to set the turn-on voltage of the transistors (threshold voltage) to the correct value.

## Slide 20: Making Transistors
3. Etch the poly
4. Implant source and drain
5. Coat the top of the poly and diffusion with metal to reduce resistance. (silicide)
Notice that the diffusion regions are formed in a self-aligned process. An oversized implant mask is used, but the field oxide and poly themselves actually define the diffusion regions. So, difficult alignment is avoided.

## Slide 21: Making Wires
1. Deposit insulator may be polished to make it flat
2. Etch contacts to Si fill with conductor
3. Pattern metal wires
Can repeat these steps to make multiple levels of metal

## Slide 22: Layout View
Layout of cell and final cross-section. This one has well contacts. In this cross section the M1 oxide was not planarized (polished flat)
p+
n+
p+
n+
p+
n+

## Slide 23: Fabrication Information
Now that we know what fabrication is trying to do, how do we tell them precisely what to build?
We don’t care about the real details of the fab, but we have to define the patterning of the layers (that meet their rules) to specify our design.
Sometimes knowing more about the fab details is useful when you need to debug a part.
Designer
Foundry
Layout (Mask Set)
Design Rules Process Parameters

## Slide 24: + Layers
Fabrication uses a set of layers that are not natural for a designer:
  Some of these layers are really the combination of layers a designer would like to think about. For example “active” is really all the diffusion layers merged together.
  Many of these layers can be derived from other layers. For example the selects and the threshold adjust implants could be derived from the diffusion type and where poly crosses the diffusion
  So rather than working at the actual mask layers, most designers create a set of more intuitive layers for the them to work with.
Requires a CAD tool to generate the real mask layers for fabrication
  Generating the manufacturing data is called ‘tapeout’
  Can have funny design rules in design layers to make sure this process is possible

## Slide 25: Layer Choice
The layers a designer uses is generally set by the CAD tool.
Our layout editor is ‘Electric’
  Electric is quick to learn and freely available.
  object-based
  Interactive DRC checking.
  Integrated with schematic editor, network compare, place & route tools
We will use the Scalable CMOS (SCMOS) design technology with Electric (MOSIS rules)
But these notes use layout from a tool called Magic so the color scheme will be slightly different.

## Slide 26: Layer Example (Magic Color Scheme)

## Slide 27: Magic Contacts
+
+
=

## Slide 28: Fabrication Constraints on Layout
Fabrication places many constraints on the layout
We will worry about the two main types of constraints:
  Resolution constraints
      What is the smallest width feature than can be printed
      What is the smallest spacing that will guarantee no shorts
    Depends on lithography and processing steps that follow
    Resolution often depends on the smoothness of the surface
      (need to keep the image in focus, since depth of field is small)
      Most modern processes are planarized, to keep surface flat
  Alignment/overlap constraints
    Like printing a color picture, need to align layers to each other
    Need to choose which layer to align to
      That layer will have better registration than the others.

## Slide 29: Geometric Design Rules
Resolution
  width and spacing of lines on one layer
Alignment
  to make sure interacting layers overlap (or don’t)
  contact surround
  poly overlap of diff
  well surround of diff
  contact spacing to unrelated geometry
3
3

## Slide 30: Design Rules
Most processes have design rules that are expressed in absolute physical units
  poly width 0.3m
  poly spacing 0.3m
  metal width 0.5m
  metal spacing 0.5m
Typically not multiples of one another
Using process-specific design rules gives the densest layout but is difficult to master
We will express our design rules in lambda () units
   is half the drawn gate length (poly width)
  All other design rules are expressed in whole multiples of 
    poly width 2 , space 3 
    metal width, space 3 
  usually requires rounding up
  rules are scaled to generate masks for a variety of processes

## Slide 31: SCMOS Lambda () Design Rules
We will be using the MOSIS SCMOS design rules
  They are a simplified set of rules
  Allow you to send your designs to a number of fab lines
  Rules are based on , a type of scaling constant
   was initially 1.5 , and now it is 0.1  in advanced fab lines
Ignores some of the ways to save area (so extra conservative)
  Use only Manhattan Layouts
  Use only 90o angles
Companies regularly do design scaling, even if they don’t use the symbol 

## Slide 32: SCMOS Design Rule Highlights
Resolution rules:
LAYER WIDTH SPACE
poly 2 3
diff 3 3
metal1 3 3
metal2 3 4
nwell 10 9
cut 2 2
via 2 3
Alignment rules:
cut/via surround 1
poly overlap diff 2
poly space to diff 1
Notes:
Cut plus surround is 4 causes layout to fall on an 8 grid

## Slide 33: Pitch
Pitch is the repeat distance between objects
8 = Contacted Transistor Pitch
  Cut + PolyWidth + 2*Cut-to-Poly
6.5 = Semi-Contacted Metal1 Pitch
  (Contact + Width)/2 + Spacing
7.5 = Semi-Contacted Metal2 Pitch
  (Contact + Width)/2 + Spacing
7 = Fully-Contacted Metal1 Pitch
  Contact + Spacing
8 = Fully-Contacted Metal2 Pitch
  Contact + Spacing

## Slide 34: + Contact Rules
In SCMOS, the spacing from contacts is often slightly larger than base material
  Poly contact to poly spacing 3
  Diffusion contact to diffusion is 4
This is done so the fabricator can make the surround of the actual contact cut slightly larger than 1 if needed

## Slide 35: The Magic Number “8”
Most of the important rules for estimating the size of stick diagrams can be approximated by 8
Metal Pitch
Metal2 w/con 8
Metal1 w/con 7
Diff w/con 8 (4 wide diff)
Poly w/dif
f con 8
Poly w/con 7
Dif
f / Poly Rules
8

## Slide 36: + Hard Rules
There are two rules that don’t fit into the nice “8” approach
Well rules
  The spacing between pdiff and ndiff is 10
  While this is larger than 8, it is not a problem
  Route at least one wire between gap
Poly Contacts
ndif
f
pdif
f
16
12 > 10
looks small
but it is not
Needs 13
Y
ou don’t need to worry
about these rules at
first.
After doing some
layout, you might check
back to see if these
rules explain some of
the problems you have
been experiencing.

## Slide 37: Using the Design Rules
While the SCMOS design rules are simplified, there are still a number of rules to remember. A good way to start is to begin with a stick diagram of the cell you want to layout. Then you can use a subset of the rules to estimate what the layout will look like, and if it meets your standards you can begin the actual layout. While CAD tools make layout easier, it always a good idea to have a plan on where things go before you start.
Warning:
While layout is often (sometimes) fun to do, it easily can be become an infinite time sink – one can always find a way to shrink the cell a few more microns. You should really have a plan BEFORE you start layout, and have a set constraints you are trying to achieve so you know when you are done.

## Slide 38: Stick Diagrams
A stick diagram is like a layout:
  Contains the basic topology of the circuit
  The relative positions of the objects are roughly correct
    Transistor 1 is to the right of transistor 2, and under transistor 3
  Each wire is assigned a layer, and crossing wires must be on different layers
But
  Wires are drawn as stick figures with no width
  The size of the objects is not to scale
  If you forgot a wire you can squeeze it in between two other wires
  It does not have to be beautiful
No matter how good the CAD tools is, it is still faster to draw a stick diagram first with pencils and paper (not beautiful is a big win).

## Slide 39: - Layout Issues
In CMOS there are two types of diffusion
ndiff (green surrounded by hatched pwell)
  Poly crossing ndiff makes NMOS transistors
pdiff (green surrounded by dotted nwell)
  Poly crossing pdiff makes PMOS transistors
Be careful, ndiff and pdiff are different
You can’t directly connect ndiff to pdiff
  Must connect ndiff to metal and then metal to pdiff
Can’t get ndiff too close to pdiff because of wells
  Large spacing rule between ndiff and pdiff
  Means you need to group NMOS devices together and PMOS devices together

## Slide 40: Basic Layout Planning
Here are a few simple guidelines to CMOS layouts
You need to route power and ground. (in metal)
  No one will auto connect it for you.
Try to keep NMOS devices near NMOS devices and PMOS devices near PMOS devices.
  So NMOS usually are placed near Gnd, and PMOS near Vdd
Run poly vertically and diffusion horizontally, with metal1 horizontal (or the reverse, just keep them orthogonal)
  Good default layout plan
Keep diffusion wires as short as possible (just connect to transistor)
All long wires (wire that go outside a cell, for example) should be in either m1 or m2.
Try to design/layout as little stuff as possible (use repetition/tools)
  Critical issue

## Slide 41: - Typical Cell Layout Plan
Look at the Parity from Lecture1
  (note: no PMOS and no Vdd Gnd) (very unusual)
CMOS Inverter/Buffer uses same plan:
Even
Odd
A
A_b
Even Out
Odd Out
A
A_b
Vdd
Gnd

## Slide 42: - Example of Size Estimation.
Parity
CMOS Inverter has similar size estimate:
The distances shown are from a line at the center of the object (contact or wire) to the center of the next contact or wire. Remember that you are measuring from the center of each object...
8 * (3 tall +1 for space to
next cell) = 32

tall
8 * (4 wide +1 for space to
next cell) = 40

wide
A
A_b
Vdd
Gnd
14
7
7
While the actual spacing
are a little dif
ferent from
the 8 rule, I would use the
8 rule for estimates.
The
numbers will be close.

## Slide 43: Estimating Layout Area from Sticks
Draw your stick diagram
Try to find the critical length path in X and in Y
Count the number of contacted pitches
  If transistors are not minimum width, remember to take that into account
If you not happy with the answer, goto step 1 and try again.
  Else you are done, and you can try to layout the cell.
You will sometimes find out that you missed the real critical length path, but that is not unusual for people starting layout. You will get better at seeing the critical path as you do more layout.

## Slide 44: - Size Estimation
If the PMOS devices are 16 wide and NMOS at 8wide
Need to add (transistor width - 4) to previous estimates, so if we were going to use the rule of 8, we would get 8 + 16 + 8 like before, plus 12 (16 - 4) plus 4 (8 - 4), or 48.
A
A_b
Vdd
Gnd
14
7
7
12
4