## Slide 1: Introduction to CMOS VLSI Design Lecture 0: Introduction
David Harris
Harvey Mudd College
Spring 2007

## Slide 2: Administrivia
Name Tents
Syllabus
  About the Instructor
  Office Hours & Lab Assistant Hours
  Textbook
  Labs, Problem Sets, and Project
  Grading
  Collaboration

## Slide 3: Introduction
Integrated circuits: many transistors on one chip.
Very Large Scale Integration (VLSI): bucketloads!
Complementary Metal Oxide Semiconductor
  Fast, cheap, low power transistors
Today: How to build your own simple CMOS chip
  CMOS transistors
  Building logic gates from transistors
  Transistor layout and fabrication
Rest of the course: How to build a good CMOS chip

## Slide 4: Silicon Lattice
Transistors are built on a silicon substrate
Silicon is a Group IV material
Forms crystal lattice with bonds to four neighbors

## Slide 5: Dopants
Silicon is a semiconductor
Pure silicon has no free carriers and conducts poorly
Adding dopants increases the conductivity
Group V: extra electron (n-type)
Group III: missing electron, called hole (p-type)

## Slide 6: p-n Junctions
A junction between p-type and n-type semiconductor forms a diode.
Current flows only in one direction

## Slide 7: nMOS Transistor
Four terminals: gate, source, drain, body
Gate – oxide – body stack looks like a capacitor
  Gate and body are conductors
  SiO2 (oxide) is a very good insulator
  Called metal – oxide – semiconductor (MOS) capacitor
  Even though gate is
  no longer made of metal

## Slide 8: nMOS Operation
Body is usually tied to ground (0 V)
When the gate is at a low voltage:
  P-type body is at low voltage
  Source-body and drain-body diodes are OFF
  No current flows, transistor is OFF

## Slide 9: nMOS Operation Cont.
When the gate is at a high voltage:
  Positive charge on gate of MOS capacitor
  Negative charge attracted to body
  Inverts a channel under gate to n-type
  Now current can flow through n-type silicon from source through channel to drain, transistor is ON

## Slide 10: pMOS Transistor
Similar, but doping and voltages reversed
  Body tied to high voltage (VDD)
  Gate low: transistor ON
  Gate high: transistor OFF
  Bubble indicates inverted behavior

## Slide 11: Power Supply Voltage
GND = 0 V
In 1980’s, VDD = 5V
VDD has decreased in modern processes
  High VDD would damage modern tiny transistors
  Lower VDD saves power
VDD = 3.3, 2.5, 1.8, 1.5, 1.2, 1.0, …

## Slide 12: Transistors as Switches
We can view MOS transistors as electrically controlled switches
Voltage at gate controls path from source to drain

## Slide 13: CMOS Inverter
A | Y
0 | 
1 | 

## Slide 14: CMOS Inverter
A | Y
0 | 
1 | 0

## Slide 15: CMOS Inverter
A | Y
0 | 1
1 | 0

## Slide 16: CMOS NAND Gate
A | B | Y
0 | 0 | 
0 | 1 | 
1 | 0 | 
1 | 1 | 

## Slide 17: CMOS NAND Gate
A | B | Y
0 | 0 | 1
0 | 1 | 
1 | 0 | 
1 | 1 | 

## Slide 18: CMOS NAND Gate
A | B | Y
0 | 0 | 1
0 | 1 | 1
1 | 0 | 
1 | 1 | 

## Slide 19: CMOS NAND Gate
A | B | Y
0 | 0 | 1
0 | 1 | 1
1 | 0 | 1
1 | 1 | 

## Slide 20: CMOS NAND Gate
A | B | Y
0 | 0 | 1
0 | 1 | 1
1 | 0 | 1
1 | 1 | 0

## Slide 21: CMOS NOR Gate
A | B | Y
0 | 0 | 1
0 | 1 | 0
1 | 0 | 0
1 | 1 | 0

## Slide 22: 3-input NAND Gate
Y pulls low if ALL inputs are 1
Y pulls high if ANY input is 0

## Slide 23: 3-input NAND Gate
Y pulls low if ALL inputs are 1
Y pulls high if ANY input is 0

## Slide 24: CMOS Fabrication
CMOS transistors are fabricated on silicon wafer
Lithography process similar to printing press
On each step, different materials are deposited or etched
Easiest to understand by viewing both top and cross-section of wafer in a simplified manufacturing process

## Slide 25: Inverter Cross-section
Typically use p-type substrate for nMOS transistors
Requires n-well for body of pMOS transistors

## Slide 26: Well and Substrate Taps
Substrate must be tied to GND and n-well to VDD
Metal to lightly-doped semiconductor forms poor connection called Shottky Diode
Use heavily doped well and substrate contacts / taps

## Slide 27: Inverter Mask Set
Transistors and wires are defined by masks
Cross-section taken along dashed line

## Slide 28: Detailed Mask Views
Six masks
  n-well
  Polysilicon
  n+ diffusion
  p+ diffusion
  Contact
  Metal

## Slide 29: Fabrication Steps
Start with blank wafer
Build inverter from the bottom up
First step will be to form the n-well
  Cover wafer with protective layer of SiO2 (oxide)
  Remove layer where n-well should be built
  Implant or diffuse n dopants into exposed wafer
  Strip off SiO2

## Slide 30: Oxidation
Grow SiO2 on top of Si wafer
  900 – 1200 C with H2O or O2 in oxidation furnace

## Slide 31: Photoresist
Spin on photoresist
  Photoresist is a light-sensitive organic polymer
  Softens where exposed to light

## Slide 32: Lithography
Expose photoresist through n-well mask
Strip off exposed photoresist

## Slide 33: Etch
Etch oxide with hydrofluoric acid (HF)
  Seeps through skin and eats bone; nasty stuff!!!
Only attacks oxide where resist has been exposed

## Slide 34: Strip Photoresist
Strip off remaining photoresist
  Use mixture of acids called piranah etch
Necessary so resist doesn’t melt in next step

## Slide 35: n-well
n-well is formed with diffusion or ion implantation
Diffusion
  Place wafer in furnace with arsenic gas
  Heat until As atoms diffuse into exposed Si
Ion Implanatation
  Blast wafer with beam of As ions
  Ions blocked by SiO2, only enter exposed Si

## Slide 36: Strip Oxide
Strip off the remaining oxide using HF
Back to bare wafer with n-well
Subsequent steps involve similar series of steps

## Slide 37: Polysilicon
Deposit very thin layer of gate oxide
  < 20 Å (6-7 atomic layers)
Chemical Vapor Deposition (CVD) of silicon layer
  Place wafer in furnace with Silane gas (SiH4)
  Forms many small crystals called polysilicon
  Heavily doped to be good conductor

## Slide 38: Polysilicon Patterning
Use same lithography process to pattern polysilicon

## Slide 39: Self-Aligned Process
Use oxide and masking to expose where n+ dopants should be diffused or implanted
N-diffusion forms nMOS source, drain, and n-well contact

## Slide 40: N-diffusion
Pattern oxide and form n+ regions
Self-aligned process where gate blocks diffusion
Polysilicon is better than metal for self-aligned gates because it doesn’t melt during later processing

## Slide 41: N-diffusion cont.
Historically dopants were diffused
Usually ion implantation today
But regions are still called diffusion

## Slide 42: N-diffusion cont.
Strip off oxide to complete patterning step

## Slide 43: P-Diffusion
Similar set of steps form p+ diffusion regions for pMOS source and drain and substrate contact

## Slide 44: Contacts
Now we need to wire together the devices
Cover chip with thick field oxide
Etch oxide where contact cuts are needed

## Slide 45: Metalization
Sputter on aluminum over whole wafer
Pattern to remove excess metal, leaving wires

## Slide 46: Layout
Chips are specified with set of masks
Minimum dimensions of masks determine transistor size (and hence speed, cost, and power)
Feature size f = distance between source and drain
  Set by minimum width of polysilicon
Feature size improves 30% every 3 years or so
Normalize for feature size when describing design rules
Express rules in terms of  = f/2
  E.g.  = 0.3 m in 0.6 m process

## Slide 47: Simplified Design Rules
Conservative rules to get you started

## Slide 48: Inverter Layout
Transistor dimensions specified as Width / Length
  Minimum size is 4 / 2sometimes called 1 unit
  In f = 0.6 m process, this is 1.2 m wide, 0.6 m long

## Slide 49: Summary
MOS transistors are stacks of gate, oxide, silicon
Act as electrically controlled switches
Build logic gates out of switches
Draw masks to specify layout of transistors
Now you know everything necessary to start designing schematics and layout for a simple chip!