## Slide 1: Introduction to CMOS VLSI Design Lecture 19: Nonideal Transistors
David Harris
Harvey Mudd College
Spring 2007

## Slide 2: Outline
Transistor I-V Review
Nonideal Transistor Behavior
  Velocity Saturation
  Channel Length Modulation
  Body Effect
  Leakage
  Temperature Sensitivity
Process and Environmental Variations
  Process Corners

## Slide 3: Ideal Transistor I-V
Shockley 1st order transistor models

## Slide 4: Ideal vs. Simulated nMOS I-V Plot
180 nm TSMC process
Ideal Models
   = 155(W/L) A/V2
  Vt = 0.4 V
  VDD = 1.8 V
BSIM 3v3 SPICE models

## Slide 5: Simulated nMOS I-V Plot
180 nm TSMC process
BSIM 3v3 SPICE models
What differs?
  Less ON current
  No square law
  Current increases
  in saturation

## Slide 6: Velocity Saturation
We assumed carrier velocity is proportional to E-field
  v = Elat = Vds/L
At high fields, this ceases to be true
  Carriers scatter off atoms
  Velocity reaches vsat
    Electrons: 6-10 x 106 cm/s
    Holes: 4-8 x 106 cm/s
  Better model

## Slide 7: Vel Sat I-V Effects
Ideal transistor ON current increases with VDD2
Velocity-saturated ON current increases with VDD
Real transistors are partially velocity saturated
  Approximate with -power law model
  Ids  VDD
  1 <  < 2 determined empirically

## Slide 8: -Power Model

## Slide 9: Channel Length Modulation
Reverse-biased p-n junctions form a depletion region
  Region between n and p with no carriers
  Width of depletion Ld region grows with reverse bias
  Leff = L – Ld
Shorter Leff gives more current
  Ids increases with Vds
  Even in saturation

## Slide 10: Chan Length Mod I-V
 = channel length modulation coefficient
  not feature size
  Empirically fit to I-V characteristics

## Slide 11: Body Effect
Vt: gate voltage necessary to invert channel
Increases if source voltage increases because source is connected to the channel
Increase in Vt with Vs is called the body effect

## Slide 12: Body Effect Model
s = surface potential at threshold
  Depends on doping level NA
  And intrinsic carrier concentration ni
 = body effect coefficient

## Slide 13: OFF Transistor Behavior
What about current in cutoff?
Simulated results
What differs?
  Current doesn’t go
  to 0 in cutoff

## Slide 14: Leakage Sources
Subthreshold conduction
  Transistors can’t abruptly turn ON or OFF
Junction leakage
  Reverse-biased PN junction diode current
Gate leakage
  Tunneling through ultrathin gate dielectric
Subthreshold leakage is the biggest source in modern transistors

## Slide 15: Subthreshold Leakage
Subthreshold leakage exponential with Vgs
n is process dependent, typically 1.4-1.5

## Slide 16: DIBL
Drain-Induced Barrier Lowering
  Drain voltage also affect Vt
  High drain voltage causes subthreshold leakage to ________.

## Slide 17: DIBL
Drain-Induced Barrier Lowering
  Drain voltage also affect Vt
  High drain voltage causes subthreshold leakage to increase.

## Slide 18: Junction Leakage
Reverse-biased p-n junctions have some leakage
Is depends on doping levels
  And area and perimeter of diffusion regions
  Typically < 1 fA/m2

## Slide 19: Gate Leakage
Carriers may tunnel thorough very thin gate oxides
Predicted tunneling current (from [Song01])
Negligible for older processes
May soon be critically important

## Slide 20: Temperature Sensitivity
Increasing temperature
  Reduces mobility
  Reduces Vt
ION ___________ with temperature
IOFF ___________ with temperature

## Slide 21: Temperature Sensitivity
Increasing temperature
  Reduces mobility
  Reduces Vt
ION decreases with temperature
IOFF increases with temperature

## Slide 22: So What?
So what if transistors are not ideal?
  They still behave like switches.
But these effects matter for…
  Supply voltage choice
  Logical effort
  Quiescent power consumption
  Pass transistors
  Temperature of operation

## Slide 23: Parameter Variation
Transistors have uncertainty in parameters
  Process: Leff, Vt, tox of nMOS and pMOS
  Vary around typical (T) values
Fast (F)
  Leff: ______
  Vt: ______
  tox: ______
Slow (S): opposite
Not all parameters are independent
for nMOS and pMOS

## Slide 24: Parameter Variation
Transistors have uncertainty in parameters
  Process: Leff, Vt, tox of nMOS and pMOS
  Vary around typical (T) values
Fast (F)
  Leff: short
  Vt: low
  tox: thin
Slow (S): opposite
Not all parameters are independent
for nMOS and pMOS

## Slide 25: Environmental Variation
VDD and T also vary in time and space
Fast:
  VDD: ____
  T: ____
Corner | Voltage | Temperature
F |  | 
T | 1.8 | 70 C
S |  | 

## Slide 26: Environmental Variation
VDD and T also vary in time and space
Fast:
  VDD: high
  T: low
Corner | Voltage | Temperature
F | 1.98 | 0 C
T | 1.8 | 70 C
S | 1.62 | 125 C

## Slide 27: Process Corners
Process corners describe worst case variations
  If a design works in all corners, it will probably work for any variation.
Describe corner with four letters (T, F, S)
  nMOS speed
  pMOS speed
  Voltage
  Temperature

## Slide 28: Important Corners
Some critical simulation corners include
Purpose | nMOS | pMOS | VDD | Temp
Cycle time |  |  |  | 
Power |  |  |  | 
Subthrehold leakage |  |  |  | 
Pseudo-nMOS |  |  |  | 

## Slide 29: Important Corners
Some critical simulation corners include
Purpose | nMOS | pMOS | VDD | Temp
Cycle time | S | S | S | S
Power | F | F | F | F
Subthrehold leakage | F | F | F | S
Pseudo-nMOS | S | F | ? | ?