## Slide 1: Introduction to CMOS VLSI Design Lecture 4: CMOS Transistor Theory
David Harris
Harvey Mudd College
Spring 2007

## Slide 2: Outline
Introduction
MOS Capacitor
nMOS I-V Characteristics
pMOS I-V Characteristics
Gate and Diffusion Capacitance

## Slide 3: Introduction
So far, we have treated transistors as ideal switches
An ON transistor passes a finite amount of current
  Depends on terminal voltages
  Derive current-voltage (I-V) relationships
Transistor gate, source, drain all have capacitance
  I = C (V/t) -> t = (C/I) V
  Capacitance and current determine speed
Also explore what a “degraded level” really means

## Slide 4: MOS Capacitor
Gate and body form MOS capacitor
Operating modes
  Accumulation
  Depletion
  Inversion

## Slide 5: Terminal Voltages
Mode of operation depends on Vg, Vd, Vs
  Vgs = Vg – Vs
  Vgd = Vg – Vd
  Vds = Vd – Vs = Vgs - Vgd
Source and drain are symmetric diffusion terminals
  By convention, source is terminal at lower voltage
  Hence Vds  0
nMOS body is grounded. First assume source is 0 too.
Three regions of operation
  Cutoff
  Linear
  Saturation

## Slide 6: nMOS Cutoff
No channel
Ids = 0

## Slide 7: nMOS Linear
Channel forms
Current flows from d to s
  e- from s to d
Ids increases with Vds
Similar to linear resistor

## Slide 8: nMOS Saturation
Channel pinches off
Ids independent of Vds
We say current saturates
Similar to current source

## Slide 9: I-V Characteristics
In Linear region, Ids depends on
  How much charge is in the channel?
  How fast is the charge moving?

## Slide 10: Channel Charge
MOS structure looks like parallel plate capacitor while operating in inversion
  Gate – oxide – channel
Qchannel =

## Slide 11: Channel Charge
MOS structure looks like parallel plate capacitor while operating in inversion
  Gate – oxide – channel
Qchannel = CV
C =

## Slide 12: Channel Charge
MOS structure looks like parallel plate capacitor while operating in inversion
  Gate – oxide – channel
Qchannel = CV
C = Cg = oxWL/tox = CoxWL
V =
Cox = ox / tox

## Slide 13: Channel Charge
MOS structure looks like parallel plate capacitor while operating in inversion
  Gate – oxide – channel
Qchannel = CV
C = Cg = oxWL/tox = CoxWL
V = Vgc – Vt = (Vgs – Vds/2) – Vt
Cox = ox / tox

## Slide 14: Carrier velocity
Charge is carried by e-
Carrier velocity v proportional to lateral E-field between source and drain
v =

## Slide 15: Carrier velocity
Charge is carried by e-
Carrier velocity v proportional to lateral E-field between source and drain
v = E  called mobility
E =

## Slide 16: Carrier velocity
Charge is carried by e-
Carrier velocity v proportional to lateral E-field between source and drain
v = E  called mobility
E = Vds/L
Time for carrier to cross channel:
  t =

## Slide 17: Carrier velocity
Charge is carried by e-
Carrier velocity v proportional to lateral E-field between source and drain
v = E  called mobility
E = Vds/L
Time for carrier to cross channel:
  t = L / v

## Slide 18: nMOS Linear I-V
Now we know
  How much charge Qchannel is in the channel
  How much time t each carrier takes to cross

## Slide 19: nMOS Linear I-V
Now we know
  How much charge Qchannel is in the channel
  How much time t each carrier takes to cross

## Slide 20: nMOS Linear I-V
Now we know
  How much charge Qchannel is in the channel
  How much time t each carrier takes to cross

## Slide 21: nMOS Saturation I-V
If Vgd < Vt, channel pinches off near drain
  When Vds > Vdsat = Vgs – Vt
Now drain voltage no longer increases current

## Slide 22: nMOS Saturation I-V
If Vgd < Vt, channel pinches off near drain
  When Vds > Vdsat = Vgs – Vt
Now drain voltage no longer increases current

## Slide 23: nMOS Saturation I-V
If Vgd < Vt, channel pinches off near drain
  When Vds > Vdsat = Vgs – Vt
Now drain voltage no longer increases current

## Slide 24: nMOS I-V Summary
Shockley 1st order transistor models

## Slide 25: Example
We will be using a 0.6 m process for your project
  From AMI Semiconductor
  tox = 100 Å
   = 350 cm2/V*s
  Vt = 0.7 V
Plot Ids vs. Vds
  Vgs = 0, 1, 2, 3, 4, 5
  Use W/L = 4/2 

## Slide 26: pMOS I-V
All dopings and voltages are inverted for pMOS
  Source is the more positive terminal
Mobility p is determined by holes
  Typically 2-3x lower than that of electrons n
  120 cm2/V•s in AMI 0.6 m process
Thus pMOS must be wider to
provide same current
  In this class, assume
  n / p = 2

## Slide 27: Capacitance
Any two conductors separated by an insulator have capacitance
Gate to channel capacitor is very important
  Creates channel charge necessary for operation
Source and drain have capacitance to body
  Across reverse-biased diodes
  Called diffusion capacitance because it is associated with source/drain diffusion

## Slide 28: Gate Capacitance
Approximate channel as connected to source
Cgs = oxWL/tox = CoxWL = CpermicronW
Cpermicron is typically about 2 fF/m

## Slide 29: Diffusion Capacitance
Csb, Cdb
Undesirable, called parasitic capacitance
Capacitance depends on area and perimeter
  Use small diffusion nodes
  Comparable to Cg
  for contacted diff
  ½ Cg for uncontacted
  Varies with process