## Slide 1: Lecture 4: Nonideal Transistor Theory

## Slide 2: Outline
Nonideal Transistor Behavior
  High Field Effects
    Mobility Degradation
    Velocity Saturation
  Channel Length Modulation
  Threshold Voltage Effects
    Body Effect
    Drain-Induced Barrier Lowering
    Short Channel Effect
  Leakage
    Subthreshold Leakage
    Gate Leakage
    Junction Leakage
Process and Environmental Variations

## Slide 3: Ideal Transistor I-V
Shockley long-channel transistor models

## Slide 4: Ideal vs. Simulated nMOS I-V Plot
65 nm IBM process, VDD = 1.0 V

## Slide 5: ON and OFF Current
Ion = Ids @ Vgs = Vds = VDD
  Saturation
Ioff = Ids @ Vgs = 0, Vds = VDD
  Cutoff

## Slide 6: Electric Fields Effects
Vertical electric field: Evert = Vgs / tox
  Attracts carriers into channel
  Long channel: Qchannel  Evert
Lateral electric field: Elat = Vds / L
  Accelerates carriers from drain to source
  Long channel: v = Elat

## Slide 7: Coffee Cart Analogy
Tired student runs from VLSI lab to coffee cart
Freshmen are pouring out of the physics lecture hall
Vds is how long you have been up
  Your velocity = fatigue × mobility
Vgs is a wind blowing you against the glass (SiO2) wall
At high Vgs, you are buffeted against the wall
  Mobility degradation
At high Vds, you scatter off freshmen, fall down, get up
  Velocity saturation
    Don’t confuse this with the saturation region

## Slide 8: Mobility Degradation
High Evert effectively reduces mobility
  Collisions with oxide interface

## Slide 9: Velocity Saturation
At high Elat, carrier velocity rolls off
  Carriers scatter off atoms in silicon lattice
  Velocity reaches vsat
    Electrons: 107 cm/s
    Holes: 8 x 106 cm/s
  Better model

## Slide 10: Vel Sat I-V Effects
Ideal transistor ON current increases with VDD2
Velocity-saturated ON current increases with VDD
Real transistors are partially velocity saturated
  Approximate with -power law model
  Ids  VDD
  1 <  < 2 determined empirically (≈ 1.3 for 65 nm)

## Slide 11: -Power Model

## Slide 12: Channel Length Modulation
Reverse-biased p-n junctions form a depletion region
  Region between n and p with no carriers
  Width of depletion Ld region grows with reverse bias
  Leff = L – Ld
Shorter Leff gives more current
  Ids increases with Vds
  Even in saturation

## Slide 13: Chan Length Mod I-V
 = channel length modulation coefficient
  not feature size
  Empirically fit to I-V characteristics

## Slide 14: Threshold Voltage Effects
Vt is Vgs for which the channel starts to invert
Ideal models assumed Vt is constant
Really depends (weakly) on almost everything else:
  Body voltage: Body Effect
  Drain voltage: Drain-Induced Barrier Lowering
  Channel length: Short Channel Effect

## Slide 15: Body Effect
Body is a fourth transistor terminal
Vsb affects the charge required to invert the channel
  Increasing Vs or decreasing Vb increases Vt
s = surface potential at threshold
  Depends on doping level NA
  And intrinsic carrier concentration ni
 = body effect coefficient

## Slide 16: Body Effect Cont.
For small source-to-body voltage, treat as linear

## Slide 17: DIBL
Electric field from drain affects channel
More pronounced in small transistors where the drain is closer to the channel
Drain-Induced Barrier Lowering
  Drain voltage also affect Vt
High drain voltage causes current to increase.

## Slide 18: Short Channel Effect
In small transistors, source/drain depletion regions extend into the channel
  Impacts the amount of charge required to invert the channel
  And thus makes Vt a function of channel length
Short channel effect: Vt increases with L
  Some processes exhibit a reverse short channel effect in which Vt decreases with L

## Slide 19: Leakage
What about current in cutoff?
Simulated results
What differs?
  Current doesn’t
  go to 0 in cutoff

## Slide 20: Leakage Sources
Subthreshold conduction
  Transistors can’t abruptly turn ON or OFF
  Dominant source in contemporary transistors
Gate leakage
  Tunneling through ultrathin gate dielectric
Junction leakage
  Reverse-biased PN junction diode current

## Slide 21: Subthreshold Leakage
Subthreshold leakage exponential with Vgs
n is process dependent
  typically 1.3-1.7
Rewrite relative to Ioff on log scale
S ≈ 100 mV/decade @ room temperature

## Slide 22: Gate Leakage
Carriers tunnel thorough very thin gate oxides
Exponentially sensitive to tox and VDD
  A and B are tech constants
  Greater for electrons
    So nMOS gates leak more
Negligible for older processes (tox > 20 Å)
Critically important at 65 nm and below (tox ≈ 10.5 Å)
From [Song01]

## Slide 23: Junction Leakage
Reverse-biased p-n junctions have some leakage
  Ordinary diode leakage
  Band-to-band tunneling (BTBT)
  Gate-induced drain leakage (GIDL)

## Slide 24: Diode Leakage
Reverse-biased p-n junctions have some leakage
At any significant negative diode voltage, ID = -Is
Is depends on doping levels
  And area and perimeter of diffusion regions
  Typically < 1 fA/m2 (negligible)

## Slide 25: Band-to-Band Tunneling
Tunneling across heavily doped p-n junctions
  Especially sidewall between drain & channel
  when halo doping is used to increase Vt
Increases junction leakage to significant levels
  Xj: sidewall junction depth
  Eg: bandgap voltage
  A, B: tech constants

## Slide 26: Gate-Induced Drain Leakage
Occurs at overlap between gate and drain
  Most pronounced when drain is at VDD, gate is at a negative voltage
  Thwarts efforts to reduce subthreshold leakage using a negative gate voltage

## Slide 27: Temperature Sensitivity
Increasing temperature
  Reduces mobility
  Reduces Vt
ION decreases with temperature
IOFF increases with temperature

## Slide 28: So What?
So what if transistors are not ideal?
  They still behave like switches.
But these effects matter for…
  Supply voltage choice
  Logical effort
  Quiescent power consumption
  Pass transistors
  Temperature of operation

## Slide 29: Parameter Variation
Transistors have uncertainty in parameters
  Process: Leff, Vt, tox of nMOS and pMOS
  Vary around typical (T) values
Fast (F)
  Leff: short
  Vt: low
  tox: thin
Slow (S): opposite
Not all parameters are independent
for nMOS and pMOS

## Slide 30: Environmental Variation
VDD and T also vary in time and space
Fast:
  VDD: high
  T: low
Corner | Voltage | Temperature
F | 1.98 | 0 C
T | 1.8 | 70 C
S | 1.62 | 125 C

## Slide 31: Process Corners
Process corners describe worst case variations
  If a design works in all corners, it will probably work for any variation.
Describe corner with four letters (T, F, S)
  nMOS speed
  pMOS speed
  Voltage
  Temperature

## Slide 32: Important Corners
Some critical simulation corners include
Purpose | nMOS | pMOS | VDD | Temp
Cycle time | S | S | S | S
Power | F | F | F | F
Subthreshold leakage | F | F | F | S